## Slide 1: Electron-Electron Interaction Driven Exotic SCs on Quasicrystals
Fan Yang (杨帆)
Beijing Institute of Technology
（北京理工大学）
2023-6-30 West Lake University, Hangzhou

## Slide 2: Collaborators
Ye Cao (BIT)
Yong-You Zhang (BIT)
Yu-Bo Liu (BIT)
Wei-Qiang Chen (SUST)
Jing Zhou(CUPT）
Congjun Wu (WLU)

## Slide 3: Outline
Introduction
Exotic SC states driven by e-e interaction on intrinsic QCs
Exotic SC states driven by e-e interaction on extrinsic QCs
Discussions & Conclusion
Y. Cao, et al, Phys. Rev. Lett. 125, 017002(2020); Y.-B. Liu, et al, Phys. Rev. B 107, 014501 (2023).
Y. Zhang, et al, SCPMA 65, 287411 (2022); Y.-B. Liu, et al, arXiv: 2301.07553 ; arXiv: 2301.06357.

## Slide 4: Outline
Introduction
Exotic SC states driven by e-e interaction on intrinsic QCs
Exotic SC states driven by e-e interaction on extrinsic QCs
Discussions & Conclusion
Y. Cao, et al, Phys. Rev. Lett. 125, 017002(2020); Y.-B. Liu, et al, Phys. Rev. B 107, 014501 (2023).
Y. Zhang, et al, SCPMA 65, 287411 (2022); Y.-B. Liu, et al, arXiv: 2301.07553 ; arXiv: 2301.06357.

## Slide 5: The QC Structure
Long-range ordered structure
A. Rotation symmetry
B. No translation symmetry
C. Projection of high-D
crystal lattice to low-D
D. Any finite-size section
repeats infinite times
The Penrose tiling
5D cubic to 2D

## Slide 6: Electron Structure of QC
Electronic state: M-I-T critical point
A. No translation symmetry: no
B. Singular smooth DOS (pseudogap, fractal)
C. Critical wave function

## Slide 7: Intrinsic QC & Extrinsic QC
Intrinsic QC: e.g. Penrose
Extrinsic QC: twisted multilayers of crystals
Examples of Ext QCs: 30o-TBG; 45o-TB cuprates
Ahn, et al., Science 361, 782–786 (2018)
W. Yao, et al, PNAS 115, 6928 (2018).
No translational period
Point group: D6d~D12
Projection of 4D crystal into 2D
Belong to extrinsic QC
The synthesized 30o-TBG
side view
top view
minimum
unit

## Slide 8: Superconductivity (SC) on QC
Superconducting Al–Zn–Mg QC
K. Kamiya, et al, Nat Commun 9:154 (2018)

## Slide 9: Fundmental Issues For SCs on QCs
What’s the pairing mechanism for SC on QC ?
How to classify pairing symmetries on QCs ?
What’s the universal properties of SCs on QCs ?
Can QCs generate novel SCs absent on crystals ?

## Slide 10: Outline
Introduction
Exotic SC states driven by e-e interaction on intrinsic QCs
Exotic SC states driven by e-e interaction on extrinsic QCs
Discussions & Conclusion
Y. Cao, et al, Phys. Rev. Lett. 125, 017002(2020); Y.-B. Liu, et al, Phys. Rev. B 107, 014501 (2023).
Y. Zhang, et al, SCPMA 65, 287411 (2022); Y.-B. Liu, et al, arXiv: 2301.07553 ; arXiv: 2301.06357.

## Slide 11: Background & Questions
Unconventional SCs driven by repulsive interactions
The Kohn-Luttinger mechanism on crystals
A. The e-e interaction can be renormalized
B. The renormalized e-e interaction is anisotropic on the FS
C. Can be decomposed into various eigen channels
D. The most-negative-eigenvalue channel is realized to cause SC
E. Technically represented by RPA, FLEX, FRG......
Can the K-L mechanism be generalized to QC?
Properties of unconventional SCs on QC?
Y. Cao, et al, Phys. Rev. Lett. 125, 017002(2020)

## Slide 12: The BCS theory for SC
The Cooper instability and BCS theory
The mean-field theory
How about direct repulsive e-e interaction?
attraction
BEC
superconductivity
cooper pair
The effective attraction is mediated by electron-phonon coupling
e
e
e
e

## Slide 13: The Kohn-Luttinger Mechanism
No Mean-field SC for the +U Hubbard model
The second-order perturbative effective H
各取一个particle-hole形的激发，Wick收缩
find , so that

## Slide 14: The Kohn-Luttinger Mechanism
The Feyman’s diagram
The effective interaction

## Slide 15: The Kohn-Luttinger Mechanism
MF treatment of the effective H
The pairing symmetry: determined by
The Tc : determined by the largest
Usually lead to unconventional SC (non s-wave)

## Slide 16: The Kohn-Luttinger instability on QCs
The Hubbard model on the QC
The second-order perturbative effective H
find , so that
各取一个particle-hole形的激发，Wick收缩

## Slide 17: The Kohn-Luttinger instability on QCs
The real-space perturbative approach
取零频

## Slide 18: The Kohn-Luttinger instability on QCs
Mean-field treatment of
Linearized gap equation near Tc
function of T

## Slide 19: Classification of pairing symmetries
The gap function always has two-variables
The classification is slightly different from crystals
Gap functions with the same Tc form an IRRP of D5
: real space
or
: eigen space
Four pairing symmetries of the Penrose tiling based on IRRPs of D5

## Slide 20: Classification of pairing symmetry
Relation between pairing angular momentum and spin statistics
平移不变系统：交换两个粒子位置等价于旋转180°+平移
Pauli’s exclusion principle:
单态：空间角动量是偶数
三重态：空间角动量是奇数

## Slide 21: Classification of pairing symmetry
Lack of translation symmetry on the QC
s -wave: singlet or triplet
p-wave: singlet or triplet
d-wave: singlet or triplet
h-wave: singlet or triplet
angular momentum around the lattice center
spin statistics
unrelated

## Slide 22: Topological SCs on QC
Two 2D IRRPs of D5 - : (px,py), (dx2-y2,d2xy)
Possible G-L free-energy minimum: p+ip and d+id, singlet or triplet TSC
With each rotation for i and j simultaneously,

## Slide 23: Pairing Phase diagram
Pairing phase diagram
Distinguished by phase-sensitve experiments
pairing phase diagram
contour plot of as function of i
s-wave singlet
d+id-wave triplet

## Slide 24: Spontaneous bulk current for chiral TSC
Chiral TSC on crystals: spontaneuos edge current
Chiral TSC on QCs: spontaneuos bulk current
Set A=0, spontaneous super current
crystal: current appear where the translation symmetry breaks, edge
QC: current appear everywhere as the translation symmetry breaks in the bluk!

## Slide 25: Brief Summary for Topic I
The K-L pairing mechanism generized to QC
Pairing symmetries classified by IRRPs of D5
Universal spontaneous bulk current for chiral TSC
(Rare on periodic lattices)
Y. Cao, et al, Phys. Rev. Lett. 125, 017002(2020)

## Slide 26: Outline
Introduction
Exotic SC states driven by e-e interaction on intrinsic QCs
Exotic SC states driven by e-e interaction on extrinsic QCs
Discussions & Conclusion
Y. Cao, et al, Phys. Rev. Lett. 125, 017002(2020); Y.-B. Liu, et al, Phys. Rev. B 107, 014501 (2023).
Y. Zhang, et al, SCPMA 65, 287411 (2022); Y.-B. Liu, et al, arXiv: 2301.07553 ; arXiv: 2301.06357.

## Slide 27: Main points for Topic II
The extrinsic QC: periodic in each layer
Quasi-period : reflected in weak interlayer coupling
New SC mechanism for extrinsic QC:
Monolayer SC + interlayer Josephson coupling (IJC)
Such IJC can generate various exotic SCs
A. Make chiral TSC from non-TSC
B. Charge-4e SC emerges as vestigial phase
Y.-B. Liu, et al, Phys. Rev. B 107, 014501 (2023); arXiv: 2301.07553 ; arXiv: 2301.06357.

## Slide 28: A Special Case:The 45o-TB Cuprates
Each D4 -symmetric monolayer carries d-wave SC with pairing angular momentum (PAM) L=2
The 45o-TB : forms an extrinsic QC
The two ODPs can couple through IJC
The Ginzburg-Landau theory: d+id chiral TSC
Y. Zhu, et al,
PRX2021
O. Can, et al, Nat. Phys. 17, 519(2021)

## Slide 29: Our General Theory
Take a twist bilayer. Suppose each Dn-symmetric (n=4/6) crystalline monolayer carries non-TSC with PAM L=n/2
Maximumly twist: Dnd ~D2n . Consequence of IJC?
Ground-state phase: chiral TSC (d+id (n=4) ; f+if (n=6) )
Vestigial phases: charge-4e SC & chiral metal
Based on G-L theory and combined RG/MC calculations.
Y.-B. Liu, et al, PRB 2023 ;
arXiv: 2301.07553;
arXiv: 2301.06357

## Slide 30: G-L Theory: Ground State
Pairing gap ; form factor ;amplitude
The fixed form factor for
The G-L free energy functional
,
Y.B.Liu, et al, arXiv: 2201.01656; ibid 2301.07553
+
+
+
+
-
-
-
-

## Slide 31: G-L Theory: Ground State
The first-order IJC : satisfies U(1)- and TR
Invariance of under dictates
The second-order IJC:
Minimization of free energy:
chiral d+id/f+if TSC
nematic d/f SC
determined by microscopic calc

+
+
+
+
-
-
-
-

## Slide 32: Two examples : 45o-TB cuprates; 30o-TBG
d+id TSC in 45o-TBC
n=4, L=n/2=2
f+if TSC in 30o-TBG
n=6, L=n/2=3
Results of microscopic calculations based on perturbational-band theory

## Slide 33: The Charge-4e SC
Charge-4e SC: long-sought novel SC beyond BCS
Real SC: Zero resistivity and Meissner effect
Characterized by half flux quantization : hc/4e
Many properties unknown, e.g. gapped or not?
Lack of unambiguous material realization
e
e
e
e
4e -- bound state
BEC
superconductivity with
fractionalized flux

## Slide 34: Charge-4e SC in TB-QCs
Inspired by the great idea of Prof. Congjun Wu
M. Zeng, L.-H. Hu, H.-Y. Hu, Y.-Z. You, and C. Wu, arXiv: 2102.06158
Pairing-phase fluctuations in a bilayer system
Low-energy effective Hamitonian of TB-QCs
Get the phase diagram by combined RG & MC
Physical quantities and correlations by MC
Total phase locked; relative phase fluctuate: charge-4e SC
Relative phase locked; total phase fluctuate: chiral metal

## Slide 35: Low-Energy Effective Model
Fix , set : spatial fluctuation
Focus on the phase fluctuation
The total- and relative- phase fields
Low-energy effective Hamiltonian
,
( )

## Slide 36: Low-Energy Effective Model
Symmetry operation under
Invariance of Hamiltonian H under requires
The resultant classical Hamiltonian
, : stiffness parameters
Y.B.Liu, et al, arXiv: 2301.06357

## Slide 37: Low-Energy Effective Model
Three types of vortices
Various phases and phase diagram
When T 0, all vortex--anti-vortex pairs chiral TSC
When T , determined by T and
,
vortices first unilateral proliferate: charge-4e SC
vortices first unilateral proliferate: chiral metal
half - half vortices first proliferate: normal metal
,
integer vortex
half-half vortex

## Slide 38: The RG Study
The action at temperature T
Map to the Sine-Gordan model
,
: dual vortex fields
,
,
: fugacities of three vortex fields
M. Zeng, et al, arXiv: 2102.06158

## Slide 39: One-Loop RG Phase Diagram
Y.B.Liu, et al, arXiv: 2301.06357

## Slide 40: The Monte-Carlo Study
Calculate physical quantities by Monte-Carlo
Superfluid density: , the Ising ODP:
Susceptibility , correlation function
, : the insert flux; : the free energy
M. Zeng, et al, arXiv: 2102.06158

## Slide 41: The Monte-Carlo Results
MC phase diagram
T dependences of quantities
Y.B.Liu, et al, arXiv: 2301.06357

## Slide 42: The Monte-Carlo Results
point A
point
D
Y.B.Liu, et al, arXiv: 2301.06357
MC phase diagram
Correlation functions for A and D

## Slide 43: Conclusion
SCs driven by e-e interaction on QCs investigated
For intrinsic QCs:
A. The K-L pairing mechanism applies
B. Pairing symmetries classified
C. Universal spontaneous bulk current in chiral TSCs
The extrinsic QCs:
A. Make chiral TSCs from non-TSCs
B. Realize the long-sought charge-4e SC
More exotic electron instabilities on QCs.
SDW, CDW, Spin Liquid, ......
Thanks!

## Slide 44: Classification of pairing symmetry
Breaking of Anderson's theorem
m and n dependence of : each m state will pair with all n
s-wave singlet
d+id-wave triplet

## Slide 45: Charge-4e SC in Hetostructure Bilayer
Charge-4e SC in hetostructure bilayer by IJC.
F. F. Song, et al, PRL2022
J1/2 : phase stiffness in layer 1/2
K: second-order IJC
When T 0, both layers host SC
When T , SC2 is first killed, (for J2<J1)
*2
-- quasi-ordering: charge-4e SC in layer2
-- unilateral quasi-ordering: SC1
-- Z2 fluctuation under the IJC: kill SC2
Charge-4e SC in layer 2 induced by charge-2e SC in layer 1 through IJC
Difficult in experiment detection: The half flux quantization invisible